## Slide 1: ACTIVATION FOR HIGH CaCO3 LOADED MIDDLE COMPOUND
THARINDA AMALKA
TRAINEE

## Slide 2: content
Objective
Methodology
Tests conducted
Results
Conclusion

## Slide 3: objective
Find out an optimum activation ratio(ZnO : Stearic Acid) for high CaCO3 loaded middle compound.
Dynamic property improvement.

## Slide 4: methodology
Physical properties, dynamic properties & cure characteristics were tested by varying the ZnO , Stearic acid phr values.
Variation of St. Acid from 0.5phr to 3.5phr by keeping ZnO at 5phr.
Variation of ZnO from 1phr to 5phr by keeping St. Acid at 3.5phr.
Rest of batches were planned according to the results of previous two batches.
Large scale mixing at CMP for selected test batch versions.*

## Slide 5: Test 01 results
 | control | SA 0.5 | SA 1.0 | SA 1.5 | SA 2.0 | SA 2.5 | SA 3.0 | SA 3.5
Tensile strength | 160.854 | 159.763 | 155.517 | 136.867 | 151.708 | 160.018 | 137.407 | 141.099
Tear strength | 35.437 | 33.66 | 32.384 | 31.394 | 33.474 | 35.365 | 26.4 | 32.791
Modulus(300%) | 91.06 | 99.8 | 96.658 | 97.217 | 100.251 | 102.251 | 87.4 | 91.74
Elongation | 487.5 | 432.5 | 420.25 | 391.25 | 406.25 | 403.75 | 402.5 | 397.5
Hardness | 67 | 67 | 68 | 68 | 69 | 69 | 68 | 69
SG | 1.388 | 1.386 | 1.399 | 1.393 | 1.392 | 1.39 | 1.395 | 1.388
Rebound % | 67 | 70 | 69 | 69 | 67 | 66 | 66 | 64

## Slide 6: Tensile & tear
Chart: Tensile strength
| control | SA 0.5 | SA 1.0 | SA 1.5 | SA 2.0 | SA 2.5 | SA 3.0 | SA 3.5
 | 160.854 | 159.763 | 155.517 | 136.867 | 151.708 | 160.018 | 137.407 | 141.099
Chart: Tear strength
| control | SA 0.5 | SA 1.0 | SA 1.5 | SA 2.0 | SA 2.5 | SA 3.0 | SA 3.5
 | 35.437 | 33.66 | 32.384 | 31.394 | 33.474 | 35.365 | 26.4 | 32.791

## Slide 7: Modulus & elongation
Chart: 
| control | SA 0.5 | SA 1.0 | SA 1.5 | SA 2.0 | SA 2.5 | SA 3.0 | SA 3.5
elongation | 487.5 | 432.5 | 420.25 | 391.25 | 406.25 | 403.75 | 402.5 | 397.5
modulus | 91.06 | 99.8 | 96.658 | 97.217 | 100.251 | 102.251 | 87.4 | 91.74

## Slide 8: hardness
control | SA 0.5 | SA 1.0 | SA 1.5 | SA 2.0 | SA 2.5 | SA 3.0 | SA 3.5
67 | 67 | 68 | 68 | 69 | 69 | 68 | 69
Chart: Hardness
| control | SA 0.5 | SA 1.0 | SA 1.5 | SA 2.0 | SA 2.5 | SA 3.0 | SA 3.5
Hardness | 67 | 67 | 68 | 68 | 69 | 69 | 68 | 69

## Slide 9: Rebound %
Chart: Rebound
| control | SA 0.5 | SA 1.0 | SA 1.5 | SA 2.0 | SA 2.5 | SA 3.0 | SA 3.5
Rebound | 67 | 70 | 69 | 69 | 67 | 66 | 66 | 64
control | SA 0.5 | SA 1.0 | SA 1.5 | SA 2.0 | SA 2.5 | SA 3.0 | SA 3.5
67 | 70 | 69 | 69 | 67 | 66 | 66 | 64

## Slide 10: Rheological properties
Chart: 
| control | SA 0.5 | SA 1.0 | SA 1.5 | SA 2.0 | SA 2.5 | SA 3.5
MH | 100.54 | 113.98 | 122.85 | 117.78 | 113.65 | 107.86 | 100.08
ML | 12.94 | 16.22 | 15.04 | 15.6 | 13.47 | 13.66 | 11.59
TS2 | 6.2 | 7.13 | 7.02 | 6.27 | 6.23 | 6.35 | 6.14
T90 | 13.24 | 14.39 | 12.46 | 12.06 | 13.16 | 12.35 | 12.07
Batch | MH | ML | TS2 | T90 | MH-ML
control | 100.54 | 12.94 | 6.2 | 13.24 | 87.6
SA 0.5 | 113.98 | 16.22 | 7.13 | 14.39 | 97.76
SA 1.0 | 122.85 | 15.04 | 7.02 | 12.46 | 107.81
SA 1.5 | 117.78 | 15.6 | 6.27 | 12.06 | 102.18
SA 2.0 | 113.65 | 13.47 | 6.23 | 13.16 | 100.18
SA 2.5 | 107.86 | 13.66 | 6.35 | 12.35 | 94.2
SA 3.5 | 100.08 | 11.59 | 6.14 | 12.07 | 88.49

## Slide 11: Blow out test results
 | Blow time | Peak temperature
Control | 59.2 | 176
SA 0.5 | 61.6 | 160
SA 1.0 | 42.7 | 158
SA 1.5 | 60.9 | 156
SA 2.0 | 53.8 | 170
SA 2.5 | 32.6 | 154
SA 3.0 | 54.1 | 178
SA 3.5 | 42.7 | 169
Chart: Blow time
| Control | SA 0.5 | SA 1.0 | SA 1.5 | SA 2.0 | SA 2.5 | SA 3.0 | SA 3.5
Blow time | 59.2 | 61.6 | 42.7 | 60.9 | 53.8 | 32.6 | 54.1 | 42.7

## Slide 12: Heat build up test results
 | Heat buildup | Initial temp | Final temp
Control | 12.94 | 93.16 | 106.1
SA 0.5 | 13.22 | 92.58 | 105.8
SA 1.0 | 12.77 | 93.13 | 105.9
SA 1.5 | 13 | 92.9 | 105.9
SA 2.0 | 13.96 | 92.04 | 106
SA 2.5 | 13.83 | 92.57 | 106.4
SA 3.0 | 15.08 | 93.02 | 108.1
SA 3.5 | 14.62 | 93.08 | 107.7
Chart: Heat buildup
| Control | SA 0.5 | SA 1.0 | SA 1.5 | SA 2.0 | SA 2.5 | SA 3.0 | SA 3.5
Heat buildup | 12.94 | 13.22 | 12.77 | 13 | 13.96 | 13.83 | 15.08 | 14.62

## Slide 13: Mooney viscosity
 | MI | MF
Control | 72.2 | 53.8
SA 0.5 | 91.03 | 64.41
SA 1.0 | 87.73 | 60.38
SA 1.5 | 31.69 | 55.8
SA 2.0 | 97.2 | 56.04
SA 2.5 | 82.79 | 54.87
SA 3.0 | 76.77 | 50.52
SA 3.5 | 70.33 | 48.63
Chart: 
| Control | SA 0.5 | SA 1.0 | SA 1.5 | SA 2.0 | SA 2.5 | SA 3.0 | SA 3.5
MI | 72.2 | 91.03 | 87.73 | 31.69 | 97.2 | 82.79 | 76.77 | 70.33
MF | 53.8 | 64.41 | 60.38 | 55.8 | 56.04 | 54.87 | 50.52 | 48.63

## Slide 14: Test 01 conclusion
Tensile strength decreased up to stearic acid 1.5PHR & with the 2.5, 3.5 PHR, tensile strength increased again.
Same kind of variation can be observe in Tear strength.
Can’t observe any significant variation in 300% modulus by increasing stearic acid PHR.
Elongation is decreased.
No any significant difference in hardness and SG values.
TS2 decreased.

## Slide 15: Test 02 results
 | ZnO 1.0 | ZnO 2.0 | ZnO 2.5 | ZnO 3.0 | ZnO 3.5 | ZnO 4.0 | ZnO 5.0
Tensile strength | 144.811 | 144.824 | 149.201 | 148.846 | 145.055 | 144.819 | 146.405
Tear strength | 27.69 | 35.538 | 33.607 | 37.043 | 31.455 | 30.653 | 30.638
Modulus(300%) | 45.552 | 79.657 | 90.995 | 91.505 | 93.65 | 90.744 | 92.23
Elongation | 560 | 430 | 415 | 417.5 | 395 | 411.67 | 397.5
Hardness | 54 | 66 | 67 | 67 | 68 | 68 | 67
SG | 1.368 | 1.371 | 1.371 | 1.373 | 1.38 | 1.38 | 1.371
Rebound % | 64 | 66 | 66 | 66 | 67 | 67 | 66

## Slide 16: Tensile & tear strength
Chart: Tensile strength
| ZnO 1.0 | ZnO 2.0 | ZnO 2.5 | ZnO 3.0 | ZnO 3.5 | ZnO 4.0 | ZnO 5.0
Tensile strength | 144.811 | 144.824 | 149.201 | 148.846 | 145.055 | 144.819 | 146.405
Chart: Tear strength
| ZnO 1.0 | ZnO 2.0 | ZnO 2.5 | ZnO 3.0 | ZnO 3.5 | ZnO 4.0 | ZnO 5.0
Tear strength | 27.69 | 35.538 | 33.607 | 37.043 | 31.455 | 30.653 | 30.638

## Slide 17: Modulus & elongation
Chart: 
| ZnO 1.0 | ZnO 2.0 | ZnO 2.5 | ZnO 3.0 | ZnO 3.5 | ZnO 4.0 | ZnO 5.0
Modulus | 45.552 | 79.657 | 90.995 | 91.505 | 93.65 | 90.744 | 92.23
Elongation | 560 | 430 | 415 | 417.5 | 395 | 411.67 | 397.5

## Slide 18: hardness
Chart: Hardness
| ZnO 1.0 | ZnO 2.0 | ZnO 2.5 | ZnO 3.0 | ZnO 3.5 | ZnO 4.0 | ZnO 5.0
hardness | 54 | 66 | 67 | 67 | 68 | 68 | 67
ZnO 1.0 | ZnO 2.0 | ZnO 2.5 | ZnO 3.0 | ZnO 3.5 | ZnO 4.0 | ZnO 5.0
54 | 66 | 67 | 67 | 68 | 68 | 67

## Slide 19: Rebound
Chart: Rebound
| ZnO 1.0 | ZnO 2.0 | ZnO 2.5 | ZnO 3.0 | ZnO 3.5 | ZnO 4.0 | ZnO 5.0
Rebound | 64 | 66 | 66 | 66 | 67 | 67 | 66
ZnO 1.0 | ZnO 2.0 | ZnO 2.5 | ZnO 3.0 | ZnO 3.5 | ZnO 4.0 | ZnO 5.0
64 | 66 | 66 | 66 | 67 | 67 | 66

## Slide 20: Rheological properties
Batch | MH | ML | TS2 | T90 | MH-ML
ZnO 1.0 | 89.79 | 12.35 | 5.53 | 9.12 | 77.44
ZnO 2.0 | 100.95 | 12.1 | 6.04 | 10.11 | 88.85
ZnO 2.5 | 101.53 | 13.4 | 5.53 | 9.39 | 88.13
ZnO 3.0 | 101.58 | 13.4 | 5.53 | 9.28 | 88.18
ZnO 3.5 | 103.87 | 13.42 | 5.54 | 9.32 | 90.45
ZnO 4.0 | 103.06 | 13.61 | 5.58 | 10.48 | 89.45
ZnO 5.0 | 105.84 | 13.63 | 5.53 | 9.49 | 92.21
Chart: 
| ZnO 1.0 | ZnO 2.0 | ZnO 2.5 | ZnO 3.0 | ZnO 3.5 | ZnO 4.0 | ZnO 5.0
MH | 89.79 | 100.95 | 101.53 | 101.58 | 103.87 | 103.06 | 105.84
ML | 12.35 | 12.1 | 13.4 | 13.4 | 13.42 | 13.61 | 13.63
TS2 | 5.53 | 6.04 | 5.53 | 5.53 | 5.54 | 5.58 | 5.53
T90 | 9.12 | 10.11 | 9.39 | 9.28 | 9.32 | 10.48 | 9.49

## Slide 21: Blow out test
 | Blow time | Peak temperature
ZnO 1.0 | 2.8 | 167
ZnO 2.0 | 7.2 | 147
ZnO 2.5 | 27 | 173
ZnO 3.0 | 37.1 | 163
ZnO 3.5 | 37.5 | 163
ZnO 4.0 | 35.4 | 160
ZnO 5.0 | 50.5 | 177
Chart: Blow time
| ZnO 1.0 | ZnO 2.0 | ZnO 2.5 | ZnO 3.0 | ZnO 3.5 | ZnO 4.0 | ZnO 5.0
Blow time | 2.8 | 7.2 | 27 | 37.1 | 37.5 | 35.4 | 50.5

## Slide 22: Heat build up test
 | Heat builup | Initial Temp | Final Temp
ZnO 1.0 | 33.67 | 93.03 | 126.7
ZnO 2.0 | 16.26 | 93.14 | 109.4
ZnO 2.5 | 16.14 | 92.06 | 108.2
ZnO 3.0 | 15.44 | 92.36 | 107.8
ZnO 3.5 | 16.15 | 92.45 | 108.6
ZnO 4.0 | 15.6 | 93.4 | 109
ZnO 5.0 | 15.17 | 93.33 | 108.5
Chart: Heat buildup
| ZnO 1.0 | ZnO 2.0 | ZnO 2.5 | ZnO 3.0 | ZnO 3.5 | ZnO 4.0 | ZnO 5.0
Heat buildup | 33.67 | 16.26 | 16.14 | 15.44 | 16.15 | 15.6 | 15.17

## Slide 23: Mooney viscosity
 | MI | ML
ZnO 1.0 | 76.67 | 49.76
ZnO 2.0 | 69.37 | 46.85
ZnO 2.5 | 73.09 | 47.67
ZnO 3.0 | 79.53 | 49.36
ZnO 3.5 | 73.42 | 49.62
ZnO 4.0 | 83.9 | 49.24
ZnO 5.0 | 76.92 | 49.2
Chart: 
| ZnO 1.0 | ZnO 2.0 | ZnO 2.5 | ZnO 3.0 | ZnO 3.5 | ZnO 4.0 | ZnO 5.0
MI | 76.67 | 69.37 | 73.09 | 79.53 | 73.42 | 83.9 | 76.92
ML | 49.76 | 46.85 | 47.67 | 49.36 | 49.62 | 49.24 | 49.2

## Slide 24: Test 02
Tensile strength is deceased with 3.5PHR stearic acid with compared to previous batch series.
As the ZnO phr increases ,Blow out time is increased.
As the ZnO phr increases, Heat buildup decreased.
When considering these two batch series, ZnO PHR values should be higher than stearic acid PHR values in a compound to get required properties.
ZnO 5phr, Stearic acid 0.5phr batch was selected considering dynamic and physical properties.
After that, selected batch was repeated with control batch.

## Slide 25: Test 03(physical properties)
 | control | ZnO 5 SA 0.5 | ZnO 5 SA 5
Tensile strength | 156.918 | 146.874 | 140.803
Tear strength | 33.891 | 36.394 | 34.698
Modulus(300%) | 96.591 | 97.211 | 92.255
Elongation | 407.5 | 385 | 385
Hardness | 67 | 68 | 68
SG | 1.387 | 1.396 | 1.386
Rebound % | 67 | 68 | 62

## Slide 26: Rheological properties
Batch | MH | ML | TS2 | T90
Control | 106.69 | 15.35 | 5.32 | 14.49
SA 0.5 | 117.38 | 17.96 | 6.38 | 15.27
SA 5.0 | 89.3 | 12.11 | 4.33 | 13.43
MH-ML
91.34
99.42
77.19

## Slide 27: Blow out & hbu results
 | Blow time | Peak temperature
control | 36.1 | 171
SA 0.5 | 61.2 | 169
SA 5.0 | 32 | 177
 | Heat buildup | Initial temp | Final temp
control | 13.97 | 93.73 | 107.7
SA 0.5 | 12.45 | 92.45 | 104.9
SA 5.0 | 19.62 | 91.88 | 111.5
According to the above results, selected activation ratio was carried out for the further testing.
But the TS2(scorch time) adjustment is needed. Therefore the next step was to reduce the PVI level & decrease TS2.

## Slide 28: Test 04
 | 0.5 PVI | 0.05PVI
Tensile strength | 150.975 | 148.24
Tear strength | 36.01 | 36.06
Modulus(300%) | 109.71 | 111.74
Elongation | 375 | 373.75
Hardness | 68 | 69
SG | 1.386 | 1.392
Rebound % | 68 | 69
 | MH | ML | TS2 | T90
0.5 PVI | 112.77 | 13.33 | 3.41 | 8.37
0.05 PVI | 127.72 | 16.41 | 3.46 | 8.19
RHEOLOGICAL PROPERTIES
PHYSICAL PROPERTIES

## Slide 29: TEST 05
In this test, impact of adding reclaim rubber to the middle compound was tested. 9.8phr of Reclaim rubber added.
 | MH | ML | TS2 | T90
SA 0.5 | 114.25 | 15.97 | 3.42 | 7.59
SA 0.5(with reclaim) | 111.07 | 17.32 | 2.52 | 6.37
no SA | 119.93 | 17.18 | 3.35 | 6.45
Large scale | 122.91 | 22.85 | 3.05 | 6.43
Large scale mixing was done(MX 008) by adding Reclaim rubber with the selected activation ratio.(RDT 1187/36)

## Slide 30: Blow out & hbu results
 | Blow time | Peak temperature
control | 61.2 | 140
SA 0.5 | 33.6 | 162
no SA | 38.8 | 181
Large scale | 38.1 | 160
 | Heat buildup | Initial temp | Final temp
control | 11.82 | 92.28 | 104.1
SA 0.5 | 15.8 | 92.1 | 107.9
no SA | 15.37 | 91.83 | 107.2
Blow out results
HBU results

## Slide 31: conclusion
Most suitable activation ratio for this middle compound is ZnO : St Acid = 5phr : 0.5phr
High PHR values of St Acid, reduces both physical & dynamic properties of the compound.
Addition of Reclaim rubber to the compound showed big impact on Dynamic properties.

## Slide 32: Test 06
After that test batches were carried out as test version of SM 1045 compound. (RDT 1187)
Four test batches were mixed in lab scale mixer to observe the dynamic & physical property variation with the addition of SSPC.
SM 1045 control
RDT 1187/37C - with SSPC, ZnO:SA = 5 : 0.5
RDT 1187/38D - ZnO:SA = 5 : 0.5 (without SSPC)
RDT 1187/38E - ZnO:SA = 4.5 : 0.5(without SSPC)
RDT 1187/39 - ZnO:SA = 5 : 0.5 , Carbon black N330 added instead of N375

## Slide 33: Test results(physical properties)
 | SM 1045 | RDT 1187/37C | RDT 1187/38D | RDT 1187/38E | RDT 1187/39
Tensile | 144.3 | 141.28 | 150.1 | 157.19 | 150.41
Tear | 33.27 | 35.4 | 34.55 | 29.75 | 36.32
Modulus | 99.92 | 108.41 | 108.12 | 104.62 | 114.2
Elongation | 390 | 366.25 | 376.25 | 397.5 | 373.33
Hardness | 66 | 67 | 66 | 65 | 67
SG | 1.373 | 1.384 | 1.388 | 1.378 | 1.376

## Slide 34: Odr results
 | MH | ML | TS2 | T90
SM 1045 | 106.29 | 11.67 | 2.54 | 6.12
RDT 1187/37C | 115.61 | 18.96 | 2.58 | 6.17
RDT 1187/38D | 123.21 | 17.66 | 2.44 | 6.2
RDT 1187/38E | 118.25 | 16.79 | 3 | 6.22
RDT 1187/39 | 121.9 | 16.92 | 2.57 | 6.19

## Slide 35: Blow out & hbu
 | Blow time | Peak temp
SM 1045 | 47 | 169
RDT 1187/37C | 61 | 159
RDT 1187/38D | 60.9 | 140
RDT 1187/38E | 60.5 | 136
RDT 1187/39 | 55.6 | 172
 | HBU
SM 1045 | 10
RDT 1187/37C | 10
RDT 1187/38D | 8
RDT 1187/38E | 8
RDT 1187/39 | 9
Chart: Blow out time
| SM 1045 | RDT 1187/37C | RDT 1187/38D | RDT 1187/38E | RDT 1187/39
 | 47 | 61 | 60.9 | 60.5 | 55.6
Chart: HBU
| SM 1045 | RDT 1187/37C | RDT 1187/38D | RDT 1187/38E | RDT 1187/39
 | 10 | 10 | 8 | 8 | 9

## Slide 36: TEST 07
Another four test batches were planned after analyzing the previous test results. Large scale mixing done at CMP MX 004. FB mixing done at MX 008.
SM 1045 control
RDT 1187/38D - ZnO:SA = 5 : 0.5
RDT 1187/38D2 - ZnO:SA = 4 : 0.5
RDT 1187/38E2 - ZnO:SA = 4.3 : 0.5
RDT 1187/40 - 3phr of Reclaim
Tire building by using these five solid middle compounds were done at ETD 2.

## Slide 37: TEST RESULTS PHYSICAL PROPERTIES (Mb - cmP & fb – LAB)
 | SM 1045 control | RDT 1187/38D | RDT 1187/38D2 | RDT 1187/38E2 | RDT 1187/40
Tensile | 145.23 | 163.07 | 160.63 | 155.76 | 145.09
Tear | 32.92 | 34.54 | 34.98 | 39.47 | 32.05
Modulus | 106.73 | 108.42 | 103.32 | 96.76 | 105.12
Elongation | 382.5 | 411.3 | 408.8 | 415 | 375
Hardness | 68 | 68 | 67 | 65 | 67
SG | 1.339 | 1.375 | 1.364 | 1.356 | 1.361

## Slide 38: PHYSICAL PROPERTIES(BOTH MB & FB AT CMP)
 | SM 1045 control | RDT 1187/38D | RDT 1187/38D2 | RDT 1187/38E2 | RDT 1187/40
Tensile | 148.57 | 159.82 | 181.31 | 174.65 | 143.63
Tear | 36.29 | 36.88 | 35.38 | 37.22 | 33.87
Modulus | 110.16 | 110.73 | 108.75 | 100.96 | 117.63
Elongation | 371.66 | 391.6 | 425 | 437.5 | 363.3
Hardness | 66 | 67 | 67 | 66 | 68
SG | 1.352 | 1.385 | 1.379 | 1.369 | 1.37

## Slide 39: Odr results
 | MH | ML | TS2 | T90 | MH - ML
SM 1045 control | 109.69 | 20.85 | 2.45 | 5.48 | 88.84
RDT 1187/38D | 133.08 | 22.45 | 3.06 | 6.41 | 110.63
RDT 1187/38D2 | 129.89 | 23.08 | 2.34 | 6.48 | 106.81
RDT 1187/38E2 | 116.53 | 22.43 | 2.45 | 6.04 | 94.1
RDT 1187/40 | 141.39 | 21.94 | 2.38 | 6.37 | 119.45
Chart: 
| SM 1045 control | RDT 1187/38D | RDT 1187/38D2 | RDT 1187/38E2 | RDT 1187/40
 | 109.69 | 133.08 | 129.89 | 116.53 | 141.39
 | 20.85 | 22.45 | 23.08 | 22.43 | 21.94
 | 2.45 | 3.06 | 2.34 | 2.45 | 2.38
 | 5.48 | 6.41 | 6.48 | 6.04 | 6.37

## Slide 40: Mooney viscosity
 | MI | MF
SM 1045 control | 124.24 | 72.69
RDT 1187/38D | 105.94 | 80.1
RDT 1187/38D2 | 104.13 | 79.99
RDT 1187/38E2 | 102.66 | 77.91
RDT 1187/40 | 104.54 | 77.65

## Slide 41: Blow out & hbu
 | Blow time | Peak temp
SM 1045 control | 36.1 | 167
RDT 1187/38D | 51.6 | 159
RDT 1187/38D2 | 67.7 | 149
RDT 1187/38E2 | 48.2 | 172
RDT 1187/40 | 61.5 | 154
 | Blow time | Peak temp
SM 1045 control | 48.9 | 173
RDT 1187/38D | 62.8 | 149
RDT 1187/38D2 | 60.9 | 141
RDT 1187/38E2 | 60.9 | 145
RDT 1187/40 | 60.1 | 128
Chart: Blow out test
| SM 1045 control | RDT 1187/38D | RDT 1187/38D2 | RDT 1187/38E2 | RDT 1187/40
FB at lab mixer | 36.1 | 51.6 | 67.7 | 48.2 | 61.5
FB at CMP | 48.9 | 62.8 | 60.9 | 60.9 | 60.1

## Slide 42: Hbu results
Chart: HBU test
| SM 1045 control | RDT 1187/38D | RDT 1187/38D2 | RDT 1187/38E2 | RDT 1187/40
FB at lab | 12 | 10 | 9 | 11 | 11
FB at CMP | 11 | 10 | 9 | 8 | 9
 | HBU
SM 1045 control | 12
RDT 1187/38D | 10
RDT 1187/38D2 | 9
RDT 1187/38E2 | 11
RDT 1187/40 | 11
 | HBU
SM 1045 control | 11
RDT 1187/38D | 10
RDT 1187/38D2 | 9
RDT 1187/38E2 | 8
RDT 1187/40 | 9

## Slide 43: Fatigue test results
 | Hours run | Temp (24hr) | Max temperature | Failure type
SM 1045 control | 34 | 165 | 198 | Air bubble in middle
RDT 1187/38D | 42 | 144 | 198 | Burst on heel area
RDT 1187/38D2 | 49.1 | 143 | 183 | Air bubble in middle
RDT 1187/38E2 | 41.2 | 152 | 180 | Air bubble in middle
RDT 1187/40 | 37 | 156 | 186 | Burst on heel area

## Slide 44: Temperature increase analysis
Chart: Run Hours
| 3 | 6 | 9 | 12 | 15 | 18 | 21 | 24 | 27 | 30 | 33 | 34
SM 1045 control | 116 | 135 | 141 | 146 | 150 | 156 | 163 | 165 | 178 | 181 | 190 | 198
RDT 1187/38D | 110 | 126 | 132 | 132 | 134 | 138 | 140 | 144 | 148 | 155 | 161 | 165 | 167 | 198
RDT 1187/38D2 | 116 | 125 | 131 | 133 | 138 | 140 | 141 | 143 | 148 | 150 | 153 | 155 | 160 | 168 | 173 | 179 | 183
RDT 1187/38E2 | 115 | 128 | 132 | 135 | 141 | 147 | 150 | 152 | 154 | 155 | 157 | 161 | 170 | 180
RDT 1187/40 | 123 | 134 | 139 | 140 | 145 | 151 | 153 | 156 | 158 | 165 | 171 | 173 | 186

## Slide 45: Conclusion
High PHR values of St Acid, reduces both physical & dynamic properties of the compound.
Addition of Reclaim rubber to the compound reduces the Dynamic properties. But small amount addition didn’t showed big impact on dynamic properties.
SSPC addition increase the heat build up of the compound.
RDT 1187/38D2 & 1187/40 versions were selected for further testing.

## Slide 46
THANK YOU!!!