## Slide 1: increase the scorch time while keeping the T90 of Rdt 1187 test version

## Slide 2: objective
Increase the scorch time(TS2) of the RDT 1187 selected test versions while keeping T90.
METHODOLOGY
Curing characteristics were tested by varying the PVI phr values. (ODR & MDR)

## Slide 3: Test 01
Large scale mixing done at CMP for selected two test versions.
2nd stage mixing was done at Lab scale mixer.
Rheological properties were tested for 0.075, 0.05 & 0.025 phr of PVI.

## Slide 4
0.075 phr of PVI
ODR results
 | MH | ML | TS2 | T90 | MH-ML
RDT 1187/40 | 117.78 | 22.57 | 3.58 | 7.44 | 95.21
RDT 1187/38D2 | 119.77 | 23.4 | 4 | 8.1 | 96.37
SM 1045 control | 108.12 | 19.96 | 2.48 | 6.19 | 88.16
Chart: ODR results
| MH | ML | TS2 | T90
RDT 1187/40 | 117.78 | 22.57 | 3.58 | 7.44
RDT 1187/38D2 | 119.77 | 23.4 | 4 | 8.1
SM 1045 control | 108.12 | 19.96 | 2.48 | 6.19

## Slide 5
0.05 phr of PVI
 | MH | ML | TS2 | T90 | MH-ML
RDT 1187/40 | 112.72 | 20.24 | 3.52 | 7.47 | 92.48
RDT 1187/38D2 | 118.72 | 20.07 | 3.52 | 8.23 | 98.65
SM 1045 control | 103.57 | 17.55 | 2.55 | 6.47 | 86.02
Chart: 
| MH | ML | TS2 | T90
RDT 1187/40 | 112.72 | 20.24 | 3.52 | 7.47
RDT 1187/38D2 | 118.72 | 20.07 | 3.52 | 8.23
SM 1045 control | 103.57 | 17.55 | 2.55 | 6.47

## Slide 6
0.025 phr of PVI
 | MH | ML | TS2 | T90 | MH-ML
RDT 1187/40 | 121.66 | 20.63 | 3.30 | 7.54 | 101.03
RDT 1187/38D2 | 117.84 | 20.91 | 3.52 | 8.38 | 96.93
Chart: 
| MH | ML | TS2 | T90
RDT 1187/40 | 121.66 | 20.63 | 3.3 | 7.54
RDT 1187/38D2 | 117.84 | 20.91 | 3.52 | 8.38
By adding 0.025phr of PVI, expected rheological properties were obtained in Lab scale 2nd stage mixing. Therefore large scale FB mixing was continued with that PVI level.

## Slide 7: Test 02
 | MH | ML | TS2 | T90
1187/38D2 (01) | 117.84 | 23.44 | 4.09 | 7.51
1187/38D2 (02) | 130.47 | 23.6 | 3.59 | 7.41
1187/40 (01) | 120.78 | 23.86 | 3.38 | 7.08
1187/40 (02) | 128.39 | 23.18 | 3.39 | 7.1
SM 1045 control (01) | 99.04 | 20.61 | 3.32 | 7.09
SM 1045 control (02) | 113.16 | 20.52 | 3.09 | 6.47
Chart: 
| 1187/38D2 (01) | 1187/38D2 (02) | 1187/40 (01) | 1187/40 (02) | SM 1045 control (01) | SM 1045 control (02)
TS2 | 4.09 | 3.59 | 3.38 | 3.39 | 3.32 | 3.09
T90 | 7.51 | 7.41 | 7.08 | 7.1 | 7.09 | 6.47

## Slide 8: Blow out & hbu results
 | Blow time | Peak temp
1187/38D2 (01) | 61.2 | 148
1187/38D2 (02) | 60.5 | 143
1187/40 (01) | 60.4 | 148
1187/40 (02) | 60.7 | 156
SM 1045 control (01) | 27.3 | 175
SM 1045 control (02) | 31.4 | 167
 | HBU
1187/38D2 (01) | 13.15
1187/38D2 (02) | 12.34
1187/40 (01) | 12.17
1187/40 (02) | 13.47
SM 1045 control (01) | 13.86
SM 1045 control (02) | 13.58

## Slide 9: conclusion
Addition of 0.025phr of PVI gives expected cure characteristics .( TS2 & T90)
PVI addition to the compound doesn’t influence to the dynamic properties of the compound.